## Slide 1: Quantum mechanical simulation of crystaline systems Roberto Dovesi Gruppo di Chimica Teorica Dip. Di Chimica IFM Università degli Studi di Torino

## Slide 2: Why simulation? Is simulation useful? Does it produce reasonable numbers? Or can only try to reproduce the experiments?
Connected question:
Is simulation expensive?

## Slide 3
How many transistors on a chip?
Gordon Moore
The number of transistors per chip doubles every 18 months
Notes: 3

## Slide 4
Performance of HPC
Notes: 4

## Slide 5: But….. The evolution of the hardware is always much faster than that of the software. Parallel computing…. How to fill supercomputers?

## Slide 6: Is simulation expensive? The last computer we bought….
Server Supermicro 64 CORE OPTERON euros 6.490 ,00
1 x Chassis 2U - 6 x SATA/SAS - 1400W
4 x CPU AMD Opteron 16-Core 6272 2,1Ghz 115W
8 x RAM 8 GB DDR3-1333 ECC Reg. (1GB/core)
1 x Backplane SAS/SATA 6 disks
1 x HDD SATAII 500 GB 7.200 RPM hot-swap
1 x SVGA Matrox G200eW 16MB
2 x LAN interface 1 Gbit
1 x Management IPMI 2.0
Cheap… but 64 cores- Parallel computing
Much less than most of the experimental equipments
64 cores enough for large calculation……..
Notes: 6

## Slide 7: At the other extreme: SUPERCOMPUTERS
Available, but:
They are fragile
Not so much standard (compiler, libreries)
c) The software (that is always late with respect to hardware) MUST BE ABLE TO EXPLOIT this huge power
Notes: 7

## Slide 8
The PRACE Tier-0 Resources
HORNET (HLRS, DE)
Cray XC30 system - 94,656 cores
CURIE (GENCI, FR)
BULL x86 system – 80,640 cores (thin nodes)
FERMI (CINECA, IT)
BlueGene Q system – 163,840 cores
SUPERMUC (LRZ, DE)
IBM System x iDataPlex system– 155,656 cores
MARENOSTRUM (BSC, SP)
IBM System x iDataPlex system– 48,448 cores
JUQUEEN (JÜLICH, DE)
BlueGene Q system – 458,752 cores

## Slide 9: MPPCRYSTAL: strong scaling
Scaling of computational time required for an SCF cycle with the number of processors for two supercells of mesoporous silica MCM-41, with a 6-31G** basis set and PBE functional. The X16 cell contains 9264 atoms and 124096 atomic orbitals, the X24 one 13896 atoms and 186144 atomic orbitals.

## Slide 10
Various approaches can be
used for the simulation of solids:
Notes: 10

## Slide 11: -classical or semi-classical energy expressions (force-field, electrostatic + repulsion terms); structural, elastic, dielectric properties of ionic and semi-ionic compounds such as Al2O3 (corundum) or SiO2 (quartz); the only available in the 1960-1980 period; still used for large systems or for a first quick determination. Parametric (then boring parametrization, usually valid for interpolation, much less for extrapolation……). -MD (molecular dynamics) based on classical mechanics (then on force fields). The only available for, say, more than 30.000 atoms (for example proteins). Temperature effect Obviously no electronic wavefunction  nothing about the related properties

## Slide 12: Quantum mechanical (based then on the solution of the Schroedinger equation at some level of approximation) a) ab initio (no parameters, also indicated as first-principle) b) semi-empirical in the quantum-mechanical frame many of the interactions (then of expensive integrals) are approximated with reference to some physical or chemical property. Cheaper than a)

## Slide 13: Quantum mechanical, ab initio I) wavefunction based (Hartree-Fock, Configuration interaction, Coupled Cluster, Moeller Plesset…..). In short: The multielectronic problem MUST be tackled through ONE electron wavefunctions: Hartree-Product >Slater Determinant >variational principle > double infinite expansion (basis set and determinants). Historically, the Molecular or Chemistry approach. Standard codes since 1960-70 (IBMOL- means IBM first explicit set of atomic wave-functions, 1974, Clementi and Roetti. Gaussian (Pople) code (1975), and others in the following years.

## Slide 14: Quantum mechanical, ab initio II) Electronic Density based (a 3 variables problem instead of 3N variables) The Hohenberg-Kohn Theorems (1964) originates the DFT (Density Functional Theory): LDA, GGA, meta-GGA, «hybrids», range separated…… a sort of medioeval «bestiarium» because: the theorems say that the TOTAL ENERGY (a number) only depends on the density (a function); however the link between the two is unknown (or known only in limiting cases as for the electron gas). In practice solves an equation very close to the one for the wavefunction.

## Slide 15: Here we consider the QUANTUM MECHANICAL ab initio approach to the properties of crystalline compounds only crystalline (means: periodic in 1, 2 3 directions)? NO! The same scheme applies to: a) local defects (say vacancies in silicon) b) desordered systems (say solid solutions)

## Slide 16: The level of the theory: non relativistic Schroedinger equation Born-Hoppeneimer approximation single particle approximation single determinant (Hartree-Fock or ….DFT) variational principle local basis set (LCAO)

## Slide 17: An obvious statement: also the simplest crystalline system is much more complicated than the simplest molecular system: Accurate studies for the latter in the ’60 (H2, methane,benzene) The first ab initio calculations for solids appear in 1979-1980 (diamond)

## Slide 18: Hystorically, two separated development lines: Molecules (or finite systems): HF based, a local basis set, all electron Solids (infinite in three directions) DFT, plane-waves, pseudopotential. In the last say 10 years…..intersections…

## Slide 19: The simulation at the theoretical chemistry group in Torino The CRYSTAL code

## Slide 20
The CRYSTAL PROJECT:
was formulated in the 1972-76 years by
Cesare Pisani, Carla Roetti and Roberto Dovesi,
starting from the periodic Hartree Fock schemes proposed
in these years by various authors
(André, Del Re, Harris, Ladik, Euwema);
first “exercices” with periodic EHT, CNDO, MNDO
Then many other contributions (local and from abroad)
Notes: 20

## Slide 21: Cesare Pisani
1938-2011
Cesare Pisani died on July 17, 2011,
in a mountains accident

## Slide 22: Carla Roetti
Carla Roetti graduated in chemistry (1967) from the University of Torino, where she became Associate Professor in Physical Chemistry in 1980.
Throughout her scientific career, she has been one of the leaders of the Theoretical Chemistry Group of the Torino University. For almost forty years (1974-2010) she has been involved with her colleagues in the quantum mechanical ab-initio study of the electronic properties of solids and in the implementation of related algorithms and computer codes, in particular of CRYSTAL.
Her contribution in this respect has been invaluable. Since the release of the first public version of CRYSTAL (1988) and throughout all the subsequent ones, she has played a leading rôle in the maintenance, portability, documentation and testing of the new features of the code, and the support of the users.
Carla Roetti has died on September 7th 2010,
all those who have worked and interacted with her deeply miss her.

## Slide 23: The CRYSTAL code for the investigation of systems periodic in 1D (polymers, nanotubes), 2D (monolayers, slabs), 3D (bulk) Born in Torino in 1976, public releases in 1988 (QCPE), 1992, 1995, 1998, 2002, 2006, 2009, 2014 Contributions from many researchers from many countries

## Slide 24: CRYSTAL88, was the first ab initio code publicly available to the scientific community, last release: 2014.

## Slide 25
The basis set consists of Bloch Functions (BF) defined in terms of local functions, the atomic orbitals (AO),  (r), throughout the entire lattice (g = lattice vector):
The local functions are, in turn, a linear combination of nG individually normalized Gaussian type functions (GTF) with constant coefficients dj and exponents j
The basis set

## Slide 26
Matrix elements of Fock matrix in direct space
Fock matrix
kinetic contribution
electron-nuclei
Coulomb el-el
exchange el-el
Integration in k space to compute the value of Fermi

## Slide 27
Hartree-Fock total energy per unit cell
The evaluation of HF total energy of a periodic system requires the evaluation of 3 infinite summations (h, g, n) that extend to all direct lattice vectors

## Slide 28
g g
h+n h+n
0 0
h h
g
h
n
g g
h+n h+n
0 0
h h
g
h
n
Coulomb integral
Exchange integral

## Slide 29
In the basis of Bloch functions the Hamiltonian matrix is factorized into diagonal blocks of finite size (the number of BFs in the unit cell), each corresponding to a point in reciprocal space.
Schrödinger equation can be solved independently at each k point.
Schrödinger equation in the BF basis
H(k) C(k) = S(k) C(k) E(k)

## Slide 30
Symmetry Adapted Crystalline Orbitals
Some k points are invariant to some point symmetry operations: this property is used to generate Symmetry Adapted Bloch Functions from a set of local functions (AO).
The method, based on the diagonalization of Dirac characters, permits to factor out H(k) into smaller diagonal blocks:

## Slide 31: The periodic model
Consistent treatment of Periodicity
  3D - Crystalline solids (230 space groups)
  2D - Films and surfaces (80 layer groups)
  1D – Polymers (75 rod groups)
  1D – Helical symmetry (up to order 48)
  0D – Molecules (32 point groups)
Infinite sums of particle interactions
  Ewald's method
  Specific formulæ for 1D, 2D, 3D
Full exploitation of symmetry
  in direct space
  in reciprocal space

## Slide 32: Hamiltonians
    Exchange functionals
    Slater [L]
    von Barth-Hedin [L]
    Becke '88 [G]
    Perdew-Wang '91 [G]
    Perdew-Burke-Ernzerhof [G]
    Revised PBE for solids [G]
    Second-order GGA expansion for solids [G]
    Wu-Cohen '06 [G]
    Correlation functionals
    Vosko-Willk-Nusair (VWN5 parameterization) [L]
    Perdew-Wang [L]
    Perdew-Zunger '81 [L]
    von Barth-Hedin [L]
    Lee-Yang-Parr [G]
    Perdew '86 [G]
    Perdew-Wang '91 [G]
    Perdew-Burke-Ernzerhof [G]
    Revised PBE for solids [G]
    Wilson-Levy '90 [G]
Restricted and Unrestricted Hartree-Fock Theory
Total and Spin Density Functional Theory
  Local functionals [L] and gradient-corrected [G] exchange-correlation functionals

## Slide 33
Types of calculations
Single-point energy calculation
Automated geometry optimization
  Full geometry optimization (cell parameters and atom coordinates)
  Freezes atoms during optimization
  Constant volume or pressure constrained geometry optimization
  Transition state search
Harmonic vibrational frequencies
  Frequencies at G point
  Phonon dispersion with an efficient supercell approach
  IR intensities through either localized Wannier functions or Berry phase scheme
  Reflectance spectrum
  Exploration of the energy and geometry along selected normal modes
Anharmonic frequencies for X-H bonds

## Slide 34: A few applications……. Total energy calculation…. Geometry optimization….

## Slide 35
CRAMBIN
Crambin is a small seed storage protein from the Abyssinian cabbage. It belongs to thionins. It has 46 aminoacids (642 atoms).
Primary structure:
Secondary structure:
N-term
C-term
α-HELIX A
α-HELIX B
β-SHEET
RANDOM COIL

## Slide 36: Tensorial Properties of Crystals
Second order
Third order
Fourth order
Dielectric
Polarizability
Piezoelectric
First hyperpolarizability
Elastic
Photoelastic
Second hyperpolarizability
Maximum number of independent elements according to crystal symmetry:
6 18 21
Minimum number of independent elements according to crystal symmetry:
1 1 3
Notes: 36

## Slide 37: Effect of the Crystal Symmetry on Tensors
Cubic
Triclinic
Third Order Tensors:
Fourth Order Tensors:
Cubic
Hexagonal
Triclinic
Hexagonal
J. F. Nye, Oxford University Press, (1985)
Notes: 37

## Slide 38: Tensorial Properties Related to Crystal Strain
Elastic Tensor
Piezoelectric Tensor
Photoelastic Tensor
Order of the Tensors
First derivative of the inverse dielectric tensor (difference with respect to the
unstrained configuration)
with respect to strain
First derivative of the polarization P (computed through the Berry phase approach) with respect to the strain
Second derivatives of the total energy E with respect to a pair of strains,
for a 3D crystal
Voigt’s notation is used according to v, u = 1, . . . 6 (1 = xx, 2 = yy, 3 = zz, 4 = yz, 5 =xz, 6 = xy) and i,j =1, 2, 3 (1 = x , 2 = y, 3 = z).
4 3 4
Notes: 38

## Slide 39
Tensorial Properties Related to Crystal Strain
Elastic Tensor
Piezoelectric Tensor
Photoelastic Tensor
Geometry definition
ELASTCON
[Optional keywords]
END
END
Basis set definition
END
Comput. Parameters
END
Geometry definition
PIEZOCON
[Optional keywords]
END
END
Basis set definition
END
Comput. Parameters
END
Geometry definition
PHOTOELA
[Optional keywords]
END
END
Basis set definition
END
Comput. Parameters
END

## Slide 40
CRYSTAL14: Elastic Properties
Pyrope-Mg3Al2(SiO4)3
A. Erba, A. Mahmoud, R. Orlando and R. Dovesi, Phys. Chem. Minerals (2013)
DOI 10.1007/s00269-013-0630-4
Notes: 40

## Slide 41
A. Erba, A. Mahmoud, R. Orlando and R. Dovesi, Phys. Chem. Minerals (2013)
DOI 10.1007/s00269-013-0630-4
CRYSTAL14: Elastic Properties
Spessartine
Grossular
Andradite
Uvarovite
Almandine
Pyrope
Elastic Anisotropy
Seismic wave velocity
Notes: 41

## Slide 42
CRYSTAL14: Piezoelectric and Dielectric Properties
A. Mahmoud, A. Erba, Kh. E. El-Kelany, M. Rérat and R. Orlando, Phys. Rev. B (2013)
Notes: 42

## Slide 43
CRYSTAL14: Photoelastic Properties
A. Erba and R. Dovesi, Phys. Rev. B 88, 045121 (2013)
The three independent elasto-optic constants of MgO, computed at PBE level, as a function of the electric field wavelength λ
p44 is almost wavelength independent
p11 and p12 show a clear dependence from λ
Dashed vertical lines in the figure identify the experimental range of
adopted electric field wavelengths
Notes: 43

## Slide 44
Vibrational properties
IR and Raman spectra……
Notes: 44

## Slide 45: Garnets: X3Y2(SiO4)3
Space Group: Ia-3d
80 atoms in the primitive cell (240 modes)
Γrid = 3A1g + 5A2g + 8Eg + 14 F1g + 14 F2g + 5A1u + 5 A2u+ 10Eu + 18F1u + 16F2u
17 IR (F1u) and 25 RAMAN (A1g, Eg, F2g) active modes
X | Y | Name
Mg | Al | Pyrope
Ca | Al | Grossular
Fe | Al | Almandine
Mn | Al | Spessartine
Ca | Fe | Andradite
Ca | Cr | Uvarovite
Notes: To illustrate vib freq calc we will use examples from garnet familly.
The generic chemical formula is X3Y2(SiO4)3.
X is a 2+ cations and Y is a 3+cation. Most of our examples are pyrope and grossluar
The eighty atoms in the primitive cell lead to 240 modes but only 17 modes are infrared active (F1u modes)
And 25 Raman modes; 3 modes are translation modes

## Slide 46
Silicate garnet spessartine structure: Mn3Al2(SiO4)3
Mn
Al
O
Si
O
O
Cubic Ia-3d
160 atoms in the UC (80 in the primitive)
O general position (48 equivalent)
Mn (24e) Al (16a) Si (24d) site positions
distorted
dodecahedra
tetrahedra
octahedra
Notes: The Garnets structure is cubic.3 types of cations sites are present
As in all silicate, silicon atoms are tetrahedraly bonded to oxygen. Tetrahedra are isolated.
Y3+ cations (as Aluminium in the grossular example) are in a octahedral environement.
X2+ cations (as Calcium in this example) is located in a distorded dodecahedra

## Slide 47
Harmonic frequency in solids with CRYSTAL
Harmonic frequencies at the central zone are obtained by diagonalising the mass weighted Hessian matrix, W
Building the Hessian matrix
analytical first derivative
numerical second derivative
Isotopic shift can be
calculated at no cost!
Notes: In order to calculate the hamonic frequency we need to build the Hessian matrix.
In a first step, the first derivative is calculated analyticaly and then derivided a second time numerical to obtain the hessian matrix
Harmonic frequencies at the central zone are obtained by diagonalising the mass weighted Hessian matrix, W.
The heavy step of these calculations is the building of the Hessian mat.
You can notice that isotopic substitution can simalated by changing the mass of atoms and rediagonalising W. This is very fast.

## Slide 48
Frequency differences (Δυ) are evaluated with respect to experimental data. υ and Δυ in cm-1.
Calculated Modes BSB |  |  | Observed Modes | 
 |  |  | Exp. a) | Exp. b)
 | υ | Δυ a) | υ | υ
F2g | 1033 | -4 | 1029 | 1027
E2g | 914 | -1 | 913 | 913
A2g | 910 | -5 | 905 | 905
F2g | 877 | 2 | 879 | 878
E2g | 852 | - | - | 892
F2g | 845 | 4 | 849 | 849
F2g | 640 | -10 | 630 | 628
E2g | 596 | -4 | 592 | 5920
F2g | 588 | -15 | 573 | 573
A2g | 561 | -9 | 552 | 550
E2g | 531 | -9 | 522 | 521
F2g | 505 | -5 | 500 | 499
F2g | 476 | -1 | 475 | 472
a) Hofmeister &Chopelas, Phys. Chem Min. 1991
b) Kolesov &Geiger, Phys. Chem. Min.1998
Spessartine raman modes : Calc vs Exp
Notes: C

## Slide 49
Frequency differences (Δυ) are evaluated with respect to experimental data. υ and Δυ in cm-1.
Spessartine raman modes : Calc vs Exp
Calculated Modes BSB |  |  | Observed Modes | 
 |  |  | Exp. a) | Exp. b)
 | υ | Δυ a) | υ | υ
E2g | 376 | -4 | 372 | 372
F2g | 366 | - | - | -
F2g | 348 | 2 | 350 | 350
A2g | 342 | 8 | 350 | 347
E2g | 320 | 1 | 321 | 318
F2g | 315 | 13 | 302 | 314
E2g | 299 | -30 | 269 | -
F2g | 221 | 0 | 221 | 229
F2g | 195 | 1 | 196 | 194
F2g | 165 | 10 | 175 | 163
E2g | 163 | -1 | 162 | 162
F2g | 105 | - | - | -

## Slide 50
Oscillator strengths of spessartine
TO freq. | Calc. f | Df | Exp. f
106.6 | 2.28 | 1.58 | 0.7
137.8 | 1.84 | 0.34 | 1.5
170.0 | 0.11 | 0.02 | 0.09
205.4 | 0.85 | 0.45 | 0.4
251.6 | 0.22 | 0.14 | 0.08
322.7 | 0.39 | 0.21 | 0.18
356.1 | 0.23 | 0.11 | 0.12
380.7 | 0.84 | -0.06 | 0.9
417.5 | 0.08 | 0.06 | 0.02
447.8 | 1.59 | 0.29 | 1.3
470.8 | 0.16 | -0.44 | 0.6
520.2 | 0.01 | -0.02 | 0.03
564.0 | 0.12 | 0.04 | 0.08
639.9 | 0.03 | 0.01 | 0.02
852.2 | 0.44 | 0.11 | 0.33
877.5 | 0.13 | 0.01 | 0.12
942.8 | 0.17 | -0.03 | 0.2
Oscillator strengths corresponding to the IR-TO modes (F1u) of spessartine.
Differences (Δf) are evaluated with respect to experimental data.
f and Δf dimensionless.
EXP Hofmeister and Chopelas, “Vibrational spectoscopy of end-member silicate garnets”, Phys. Chem. Min., 17, 503-526 (1991).
|Df|
0
0.25
0.5
2

## Slide 51: Garnets : Statistics
Statistical analysis of calculated IR and Raman modes of garnets compared to experimental data.
a) Hofmeister et al., Phys. Chem. Min. 1996. 81, 418
b) McAloon et. al., Phys. Chem. Min. 1995. 80, 1145
c) Hofmeister et. al., Phys. Chem. Min. 1991. 17, 503
d) Hofmeister, private comm.
e) Kolesov et. al., Phys. Chem. Min. 1998. 25, 142
IR frequencies
Raman frequencies(e)
Notes: To illustrate vib freq calc we will use examples from garnet familly.
The generic chemical formula is X3Y2(SiO4)3.
X is a 2+ cations and Y is a 3+cation. Most of our examples are pyrope and grossluar
The eighty atoms in the primitive cell lead to 240 modes but only 17 modes are infrared active (F1u modes)
And 25 Raman modes; 3 modes are translation modes

## Slide 52: IR reflectance spectrum
Reflectivity is calculated from dielectric constant by means of:
(θ is the beam incident angle)
The dielectric function is obtained with the classical dispersion relation:
Comparison of computed and experimental IR reflectance spectra for garnets: a) pyrope b) grossular c) almandine .
Notes: To illustrate vib freq calc we will use examples from garnet familly.
The generic chemical formula is X3Y2(SiO4)3.
X is a 2+ cations and Y is a 3+cation. Most of our examples are pyrope and grossluar
The eighty atoms in the primitive cell lead to 240 modes but only 17 modes are infrared active (F1u modes)
And 25 Raman modes; 3 modes are translation modes

## Slide 53: IR reflectance spectrum of grossular
Computed and experimental IR reflectance spectra of grossular garnet, plus imaginary parts of ε and 1/ε.
Notes: To illustrate vib freq calc we will use examples from garnet familly.
The generic chemical formula is X3Y2(SiO4)3.
X is a 2+ cations and Y is a 3+cation. Most of our examples are pyrope and grossluar
The eighty atoms in the primitive cell lead to 240 modes but only 17 modes are infrared active (F1u modes)
And 25 Raman modes; 3 modes are translation modes

## Slide 54: IR reflectance spectrum: required quantities
Optical dielectric constant e∞
  Computed through a Coupled Perturbed HF(KS) scheme
Transverse Optical vibrational frequencies n
  Eigenvalues of the Hessian matrix, constructed in the harmonic approximation
Damping factors g
  A constant value 8 cm-1 is adopted
Optical dielectric constants of garnets
(expt. from Medenbach et al., J. Opt. Soc.Am. B, 1997, 14, 3299-3318)
Notes: To illustrate vib freq calc we will use examples from garnet familly.
The generic chemical formula is X3Y2(SiO4)3.
X is a 2+ cations and Y is a 3+cation. Most of our examples are pyrope and grossluar
The eighty atoms in the primitive cell lead to 240 modes but only 17 modes are infrared active (F1u modes)
And 25 Raman modes; 3 modes are translation modes

## Slide 55
25 modes
The RAMAN spectrum of Pyrope:

## Slide 56: From A1g+Eg wavenumbers...
 |  | Ours | Hofmeister |  | Chopelas |  | Kolesov | 
Sym | M | υ (cm-1) | υ (cm-1) | Δυ (cm-1) | υ (cm-1) | Δυ (cm-1) | υ (cm-1) | Δυ (cm-1)
 | 1 | 352.5 | 362 | -10 | 362 | -10 | 364 | -12
A1g | 2 | 564.8 | 562 | 3 | 562 | 3 | 563 | 2
 | 3 | 926.0 | 925 | 1 | 925 | 1 | 928 | -2
 | 4 | 209.2 | 203 | 6 | 203 | 6 | 211 | -2
 | 5 | 308.5 |  |  | 309 | -1 | 284 | 25
 | 6 | 336.5 | 342 | -6 |  |  | 344 | -8
 | 7 | 376.9 | 365 | 12 | 379 | -2 | 375 | 2
Eg | A |  | 439 |  | 439 |  |  | 
 | 8 | 526.6 | 524 | 3 | 524 | 3 | 525 | 2
 | 9 | 636.0 | 626 | 10 | 626 | 10 | 626 | 10
 | 10 | 864.4 |  |  | 867 | -3 |  | 
 | B |  | 911 |  |  |  |  | 
 | 11 | 937.4 | 938 | -1 | 938 | -1 | 945 | -8
Frequency differences are evaluated with respect to calculated data.
Hofmeister: Hofmeister & Chopelas, Phys. Chem. Min., 1991
Chopelas: Chaplin & Price & Ross, Am. Mineral., 1998
Kolesov: Kolesov & Geiger, Phys. Chem. Min., 1998

## Slide 57: ... to RAMAN spectra!

## Slide 58: And now F2g wavenumbers...
 |  | Ours | Hofmeister |  | Chopelas |  | Kolesov | 
Sym. | M | υ (cm-1) | υ (cm-1) | Δυ (cm-1) | υ (cm-1) | Δυ (cm-1) | υ (cm-1) | Δυ (cm-1)
 | 12 | 97.9 | - | - | - | - | 135 | -37
 | 13 | 170.1 | - | - | - | - | - | -
 | 14 | 203.7 | 208 | -4 | 208 | -4 | 212 | -8
 | C |  | 230 |  | 230 |  |  | 
 | 15 | 266.9 | 272 | -5 | 272 | -5 | - | -
 | D |  | 285 |  |  |  |  | 
 | 16 | 319 | 318 | 1 | 318 | 1 | 322 | -3
F2g | E |  |  |  | 342 |  |  | 
 | 17 | 350.6 | 350 | 1 | 350 | 1 | 353 | -2
 | 18 | 381.9 | 379 | 3 | 379 | 3 | 383 | -1
 | 19 | 492.6 | 490 | 3 | 490 | 3 | 492 | 1
 | 20 | 513.5 | 510 | 4 | 510 | 4 | 512 | 2
 | 21 | 605.9 | 598 | 8 | 598 | 8 | 598 | 8
 | 22 | 655.3 | 648 | 7 | 648 | 7 | 650 | 5
 | 23 | 861 | 866 | -5 | 866 | -5 | 871 | -10
 | 24 | 896.7 | 899 | -2 | 899 | -2 | 902 | -5
 | 25 | 1068.4 | 1062 | 6 | 1062 | 6 | 1066 | 2
Frequency differences are evaluated with respect to calculated data.
Hofmeister: Hofmeister & Chopelas, Phys. Chem. Min., 1991
Chopelas: Chaplin & Price & Ross, Am. Mineral., 1998
Kolesov: Kolesov & Geiger, Phys. Chem. Min., 1998
B3LYP overstimates the lattice parameter!

## Slide 59: ... and the RAMAN spectra!
A1g peaks also in F2g spectrum caused by the presence of different crystal orientations and/or rotation of the polarized light.

## Slide 60
High-order dielectric properties of solids

## Slide 61
The total energy of a crystal in an electric field
The total energy (Etot) of a crystal (or a molecule) in a “weak” electric field () can be expressed as a perturbative series of the field components plus the total energy of the field-free system (E0tot):
dipole moment
polarizability
first-order hyperpolarizability
second-order hyperpolarizability
The effect of a low-intensity high-frequency electric field () applied to a crystal within the periodic boundary conditions can be represented by the following perturbative term in the Hamiltonian operator:
 depends on k, any point in the reciprocal space
position operator
gradient in k space

## Slide 62
Static polarizability and hyperpolarizabilities
n+1 formulation
2n+1 formulation
2n+1 formulation
substitute for U[2]

## Slide 63
Dielectric properties
Polarizability (α) and hyperpolarizability ( and  ) tensors are related to other tensors:
first-order electric susceptibility
dielectric tensor
second-order electric susceptibility
third-order electric susceptibility
second-harmonic generation (SHG) electric susceptibility
V = unit cell volume
δ = Kronecker delta

## Slide 64
TI |  | d |  | 
6 | 4.8391 | - 6.3452 | 7.2035 | 2.9887
7 | 4.8446 | - 6.3746 | 7.2796 | 3.0221
8 | 4.8420 | - 6.4141 | 7.2435 | 3.0180
10 | 4.8544 | - 6.5059 | 7.4565 | 3.1180
12 | 4.8596 | - 6.5626 | 7.5326 | 3.1548
14 | 4.8655 | - 6.6116 | 7.6932 | 3.2351
16 | 4.8669 | - 6.6225 | 7.7307 | 3.2529
18 | 4.8680 | - 6.6245 | 7.7668 | 3.2691
Dependence of α, ,  on series truncation (I)
Cubic 3C-SiC at the experimental lattice parameter
TI: tolerances for the truncation of the Coulomb and exchange series
T1=T2=T3=T4=TI T5= 2 TI
overlap < 10-TI
d in pm/V
(3) in 10-14 esu
HF approximation

## Slide 65
6.52
6.2-8.7
7.18
Experiment
5.71
+ scissors
7.45
PW-LDA-GW
8.83
PW-LDA
8.00
+ scissors
12.4
PW-LDA
15.3
5.54
5.05
HF
8.32
10.4
6.19
PBE0
8.05
10.5
6.10
B3LYP
6.26
14.8
6.85
PBE
6.32
15.0
6.85
LDA
gap
d
Static optical properties of cubic 3C-SiC
d in pm/V
gap in eV
CRYSTAL09 calculations

## Slide 66
Potassium Di-hydrogen Phosphate KDP
Chemical formula: KH2PO4
NonLinear Optic Properties (NLO):
the electric polarization (P) shows a NON LINEAR optic
response to the applied electric field (F).
Ferroelectric Phase Transition (PARA->FERRO) at 123° K
I-4d2
para
Fdd2
ferro
Fdd2
ferro

## Slide 67
Potassium Di-hydrogen Phosphate KDP
Symmetric H-bonds
Above Tc: DISORDER, protons move along the H-bond (PE)‏
Transition state as documented by negative frequencies.
  Protonic Trasfer
  Below Tc: ORDER, protons fixed in ferroelectric domains (FE)
  Real minimum: all frequencies are positive
Tetragonal (I-4d2)
Orthorhombic (Fdd2)

## Slide 68
Potassium Di-hydrogen Phosphate KDP
I-4d2 Fdd2
P
V. Lacivita, M. Rérat, B. Kirtman, M. Ferrero, R. Orlando and R. Dovesi, J. Chem. Phys. 2009.
K
I-4d2 (Exp) Fdd2 (Exp.)
a 7.44 (7.44) 10.56 (10.53)
b 7.44 (7.44) 10.67 (10.44)
c 6.95 (6.97) 6.98 ( 6.90 )
H-O1 1.19 (1.25) 1.03 ( 1.05 )
H-O2 1.19 (1.25) 1.48 ( 1.44 )
P-O1 1.54 (1.54) 1.58 ( 1.59 )
P-O2 1.54 (1.54) 1.51 ( 1.50 )
OPTGEOM: PBE0 [1]

## Slide 69
Potassium Di-hydrogen Phosphate KDP
V. Lacivita, M. Rérat, B. Kirtman, M. Ferrero, R. Orlando and R. Dovesi, J. Chem. Phys. 2009.
CPHF: B3LYP, Exp. geom.

## Slide 70
Potassium Di-hydrogen Phosphate KDP
Dielectric Tensor and Optical Indicatrix
DIAGONALIZATION ->
PRINCIPAL REFRACTIVE INDICES
(a <= b <= g)
BIREFRINGENCE: B = g - a (≠ 0)
OPTICAL CLASSES:
1) MONOAXIAL = one monorefringence direction (one optical axis)
2) BIAXIAL = two monorefringence directions (two optical axes)

## Slide 71
Potassium Di-hydrogen Phosphate KDP
Monoaxial
Oblate optical indicatrix
  Biaxial
Tetragonal (I-4d2)
Orthorhombic (Fdd2)
w
optic axis
e = 1.43
w = 1.49
a = 1.436
b = 1.476
g = 1.484
CPHF: B3LYP, Exp. geom.

## Slide 72
Nanotubes

## Slide 73
Nanotubes
Why?
What’s new in the implemented method?
Nanotube ab initio simulation is, in general, expensive:
the unit cell can contain hundreds or thousands of atoms.
The exploitation of the high point symmetry
in helical 1D systems allows to
dramatically reduce the computational cost
and automatically build nanotubes
from 2D and 3D structures.
QM ab initio calculation of nanotubes with large basis sets and
hybrid functionals: POSSIBLE AND NOT EXPENSIVE
Y. Noël, P. D’Arco, R. Demichelis, C. M. Zicovich-Wilson, R.Dovesi; J. Comput. Chem., 2010, 31, 855-862

## Slide 74
Nanotubes
Automatic Construction of a Nanotube from 2D Structures
(CRYSTAL can authomatically cut 2D layers from 3D structures)
We start from 2D graphene, a simple case ---> C nanotube (CNT).
a2
a1
R=n1a1+n2a2
Rolling direction
|R|:nanotube circumference
(n1,n2) defines the nanotube
Shortest lattice vector perpendicular to R:
L=l1a1+l2a2
* Noël, D’Arco, Demichelis, Zicovich-Wilson, Dovesi; J. Comput. Chem., 2010, 31, 855-862

## Slide 75
Nanotubes
A CNT unit cell can contain hundreds of atoms
BUT
ONLY 2 IRREDUCIBLE ATOMS WITH HELICAL SYMMETRY EXPLOITATION
Exploitation of the High Point Symmetry of Nanotubes
EXAMPLE: frequency calculation of the (24,0) SWCNT
(96 atoms in the unit cell)
FREQUENCY CALCULATION:
- equilibrium geometry
- displacement of each atom along the 3 Cartesian directions
96x3+1=289 SCF calculations
If the calculation is performed on 2 irreducible atoms:
2x3+1=7 SCF calculations (helical symmetry exploitation)
* Noël, D’Arco, Demichelis, Zicovich-Wilson, Dovesi; J. Comput. Chem., 2010, 31, 855-862

## Slide 76
Nanotubes
Exploitation of the High Point Symmetry of Nanotubes
The helical symmetry of nanotubes is then exploited at three levels:
1 - Automatic generation of the nanotube starting from a 2D structure
Build the (4,2) SWCNT
CRYSTAL
0 0 0
186
2.47 6.70
2
6 0.000000 0.000000 0.000000
6 0.333333 0.666667 0.000000
SLAB
0 0 1
1 1
SWCNT
4 2
3D geometry
Cut a slab
Build nanotube
Easy to use
Thick slabs can be treated
Geometry guess for nanotubes
* Noël, D’Arco, Demichelis, Zicovich-Wilson, Dovesi; J. Comput. Chem., 2010, 31, 855-862

## Slide 77
Nanotubes
Time Scaling
B3LYP, 6-1111G*
single processor Intel Xeon
1.86GHz, RAM 8Gb
* Noël, D’Arco, Demichelis, Zicovich-Wilson, Dovesi; J. Comput. Chem., 2010, 31, 855-862

## Slide 78
Nanotubes
Time Scaling
* Demichelis, Noël, D’Arco, Maschio, Orlando, Dovesi; submitted for publication
NANORE (SWCNTRE): build a (n1,n2) nanotube from the structure of another one
''old'' nanotube unrolled and re-rolled according to a new R vector, with minor modifications to the structure.
EXAMPLE: geometry optimisation of imogolite
Al2(OH)3SiO3OH, tubular hydrated aluminosilicate
(thick slabs, large systems, tube and slab geometries very different)
starting structure for the optimisation
(the optimised slab or a previously optimised tube)
ATOMS Beginning Number of SCF+gradient
(8,0)
(9,0)
(10,0)
(11,0)
(12,0)
224
252
280
308
336
(9,0)
(10,0)
slab
(10,0)
(11,0)
22
20
46
19
16
-47.8
-52.1
-52.6
-51.8
-50.8
-8.0
-4.2
-236.6
-2.4
-1.5
E
E
E: Energy difference with respect to slab, kJ/mol per fu
E: Energy relaxation after rigid unrolling and re-rolling , kJ/mol per fu

## Slide 79
Nanotubes
Inorganic Nanotubes: the Case of Chrysotile
“White” asbestos:
wrapping of lizardite - phyllosilicate, Mg3Si2O5(OH)4
FIRST AB INITIO SIMULATION OF SINGLE LAYER CHRYSOTILE
(smallest fibre in the nature ~1000 atoms in the unit cell)
brucite-type octahedral sheet (MgO6 octahedra sharing edges)
tetrahedral sheet (vertices-sharing SiO4 tetrahedra forming hexagonal motif)
The misfit might be one of the main responsible for chrysotile curling. Octahedral external wall is allowed to expand and tetrahedral wall to contract.
Brucite-like slab : lattice parameter 5.43 Å
SiO3(OH)2 slab : lattice parameter 5.32 Å
Lizardite slab : lattice parameter 5.37 Å
* D’Arco, Noël, Demichelis, Dovesi; J. Chem. Phys., 2009, 131, 204701

## Slide 80
FULLERENES
Notes: 80

## Slide 81: Input again: general!!

## Slide 82
C1500 fullerene
Some (in pink) hexagons (or pentagons in orange) cannot change their orientation; it is fixed by symmetry

## Slide 85: Comparison of optimized structures
C240
C540
C960
Each fullerene is compared to the C1500. The center of pentagons have been taken as reference.

## Slide 87: FULLERENES: size of the matrices
(n,n) | nat | Nat | NAO | SFIRR | SFRED | R1 | R2 | R4
(1,1) | 1 | 60 | 840 | 1759 | 169'980 | 97 | 401 | 22
(2,2) | 3 | 240 | 3360 | 6707 | 716'130 | 107 | 1683 | 23
(3,3) | 6 | 540 | 7560 | 14570 | 1'609'020 | 110 | 3923 | 23
(4,4) | 10 | 960 | 13440 | 25377 | 2'847'690 | 112 | 7118 | 23
(6,6) | 21 | 2160 | 30240 | 55661 | 6'362'370 | 114 | 16429 | 24
(8,8) | 36 | 3840 | 53760 | 97559 | 11’260’170 | 115 | 29625 | 24
(10,10) | 55 | 6000 | 84000 | 151071 | 17’541’090 | 116 | 46707 | 24
nat = number of irreducible atoms, Nat = number of atoms, NAO = number of AO
SFIR (SFRED ) = size of the irreducible (reducible) compact Fock matrix.
R1, R2 and R4 = SFRED/SFIRR , NAO2/SFIRR and NAO/MAXIR.
Nop = 120
NIR = 10

## Slide 88
 | t | (1,1) | (4,4) | (6,6) | (8,8)* | (10,10)*
A. | init | 26.36 | 64.92 | 184.54 | 418.64 | 825.41
“ | over | 81.40 | 8.11 | 22.36 | 56.73 | 135.85
B. | pole | 326.15 | 6.64 | 14.76 | 26.51 | 40.77
“ | biel | 8.34 | 154.46 | 578.06 | 1141.61 | 1885.74
“ | mono | 0.02 | 4.45 | 21.98 | 68.70 | 166.01
C. | fock | 0.16 | 7.71 | 18.91 | 36.27 | 56.31
D. | diag | 0.1 | 2.51 | 26.20 | 183.42 | 729.50
E. | dens | 1.23 | 93.02 | 233.02 | 441.63 | 740.14
F. | dft | 5.50 | 55.16 | 126.18 | 437.99 | 702.36
 | TOTcyc | 15.67 | 323.97 | 1019.14 | 2336.16 | 4320.87
 | TOTSCF | 1265.23 | 6552.43 | 20589.74 | 47198.57 | 87378.66
 | grad | 83.99 | 1253.55 | 3191.33 | 10088.28 | 16170.70
Time (in seconds): ONE CORE
construction of symmetry group and transformation matrices (init), construction of the overlap matrix (over), calculation of multipole (pole), bi- (biel) and mono- (mono) electronic integrals, transformation of f into F (fock), Fock matrix diagonalization (diag), construction and back transformation of the density matrix (dens), calculation of the electron density over the DFT grid (dft), a single SCF cycle (TOTcyc, from B. to F.), the entire SCF procedure (TOTSCF , 20 SCF cycles considered), calculation of the gradient for geometry optimization (grad). Calculations from (7,7) on (marked with an asterisk) were performed using the “low memory" option.