## Slide 1
* Corresponding author: Marco Ferrero, INFN Torino, marco.ferrero@to.infn.it
Acknowledgments
NFN - Gruppo V
Horizon 2020, grant UFSD669529
Horizon 2020, grant no. 654168 (AIDA-2020)
U.S. Department of Energy grant number DE-SC0010107
Dipartimenti di Eccellenza, Univ. of Torino (ex L. 232/2016, art. 1, cc. 314, 337)
Conclusion
Ultra-Fast Silicon Detectors are being realized in form of thin Low-gain Avalanche Detectors
Radiation hardness improved by co-implantation of carbon into the gain layer
The interplay of acceptor removal and the capability to recover the effect of fluence with Bias will determine the more radiation resistance designs.
16-17µm is the minimum inter-pads distance measured in multi-pad sensors
Trench isolation and and Resistive AC-coupling detectors are the two technological solution to improve the inactive inter-pad region in multi-pad sensors
M. Ferrero1*, R. Arcidiacono4, G. Borghi5, M. Boscardin5, N. Cartiglia1, M.Costa2, G.F. Dalla Betta3, F.Ficorella5, M. Mandurrino1, M.M. Obertino2, L. Pancheri3, G. Paternoster5, F. Siviero2, V. Sola1,2, A. Staiano1, M.Tornago2, M. Vignali5
1INFN, Torino, Italy
2Università di Torino, Torino, Italy
3Università di Trento and INFN, Dipartimento di ingegneria industriale, Trento, Italy
4Università del Piemonte Orientale, Novara, Italy
5Fondazione Bruno Kessler (FBK), Trento, Italy
Evolution of the design of Ultra Fast Silicon detector to cope with high irradiation fluences and fine segmentation
15th Topical Seminar on Innovative Particle and Radiation Detectors (IPRD19) 14-17 October 2019, Siena, Italy
UFSD standard design
Transversal cut of a standard multi pad UFSD sensor
Full
gain
region
Full
gain
region
No gain region
Trench Isolated LGADs
Trench isolation technology successfully used in FBK UHD SiPMs
Trench isolation could reduces inter-pad border region down few µm:
Typical trench width < 1µm
Trench filling with SiO2, Si3N4, Polysilicon
Transversal cut of a UFSD trench isolated sensor
Full
gain
region
Full
gain
region
No gain region
250µm
375µm
SEM imagine of a sensor with double trench isolation
SEM imagine of a sensor with single trench isolation
FBK started a first development run of TI-LGADs in 2019 to demonstrate feasibility of technological process
Front view of a two pads device
Layout splits:
n of trenches (1-2 trenches)
Guard ring isolation (trench Vs p-stop)
FBK-UFSD3 inter-pad layout (in scale)
FBK UFSD3 production (2018)- reducing the border dimensions in terminations structure
Inter-pad measured with TCT setup, using a 1064nm focused laser
UFSD3 Wafer layout
Design | Nominal distance (µm) | Measured distance (µm)
Safe | 31 | 30.4
Intermediate | 20.5 | 16.7
Aggressive | 11 | 16.4
Three different inter-pad design with different nominal distance gain layer implant:
Safe design 30µm
Intermediate design 20µm
Aggressive design 10µm
Resistive AC-Coupled Silicon Detectors (RSD)
Transversal cut of a RSD sensor
Simplified model
Full gain region
RSD1 production:
Si-Si Float Zone (FZ) and epitaxial (Epi) substrate;
three n++ doses;
two capacitive oxide thickness;
pads matrix with 50x50 to 500x500 µm2 pitch and different pads size;
2D maps of integrated charge and signal waveform induced with TCT laser (=1064nm) scan on RSDs with different pitch and pad size
3x3 pad matrix;
200µm x 200µm pitch;
150µm x 150µm pad size;
Integration time of 5ns;
3x3 pad matrix;
50µm x 50µm pitch;
25µm x 25µm pad size;
Integration time of 2.7ns;
Silicon particle detector with 100% fill factor
Safe
Intermediate
Aggressive
Low Gain avalanche Diode (LGAD)
Principle:
Add to n-on-p Silicon sensor an extra thin p-layer (1016 atoms/cm3) below the junction which increases the E-field so that charge multiplication with moderate gain of 10-50 occurs without breakdown.
High Doping Concentration equal High Field
Ultra Fast Silicon Detector (UFSD) is a thin LGAD (50µm thick) optimized to achieve a time resolution of 0ps
Radiation effects
Acceptor removal
(gain layer effect)
c(NA(0)) acceptor removal coefficient
Acceptor creation
(bulk effect)
geff cm-1
Acceptor creation
Acceptor removal
+
Acceptor removal
LGAD gain mechanism
Thinner and Higher gain layer profiles are more radiation resistance
Acceptor removal mechanism is mitigated by co-implantation of carbon into gain layer
Neutron
irradiation
Investigation of acceptor removal mechanism on different gain layer flavors
Proton
irradiation
cn (B LD + C_A)
cn (B HD + C_A)
Proton irradiation induces more or equal acceptor removal than Neutron
Effect of Proton energy: acceptor removal is faster for lower Proton energy
Dependence of acceptor removal upon the proton energy
Very low current <100pA;
Breakdown due to internal gain at 350V;
No Breakdown up to 400V in sensors without gain;
Full depletion capacitance 0.2pF as expected;
Perfect pads electrical insulation;
4D tracking motivation
Timing-Tracking capability is strongly motivated by high dense environments in future hadron collider
Sensors requirements:
Radiation resistance
High fill factor (fraction of active area)
Bunch crossing simulation HL-LHC
Ultra fast silicon detectors (UFSDs) are suitable for 4D tracking in future experiments at HL-LHC:
Time resolution of 30ps
Segmentable electrodes;
Performances maintained at fluences > 1015 neq/cm2
UFSD design based on Low Gain Avalanche diode technology
Chart: Doping distribution n++ electrode and Gain layer
n++ implant
Gain layer
p+ implant
High Electric field drift space
Q1
E1
d1
Q2
E2
d2
Shallow GL
Deep GL
n implant
Gain layer
p implant
Bulk
Deep Gain Layer (DGL)
Shallow Gain Layer (SGL)
Gain: exp(field * distance)
Shallow gain layers work at higher E field.
Multiplication in the Bulk: ~ 170-200 kV/cm
Deep Gain Layer: ~ 290 – 300 kV/cm
Shallow Gain Layer: ~ 380 – 400 kV/cm
The position of the GL determines the field working point: the deeper it is, the lower the field is
Depth
Different manufacturers have different gain layer strategies:
FBK: shallow implant
HPK: deep implant
At high field the mean free path is saturated, so the “recovering power” of bias is much reduced. At lower field, bias is more effective